Specification for Aluminum Base Foil: 

Description: Clear, smooth, non-toxic, rigid Aluminum Foil.
Dimension:  
       i) Width -         176 mm ± 5mm

      ii) Thickness -   0.15 ± 0.05 mm
Gram mage:   240 to 280 GSM
Pinhole Test: It should not have any pinholes.

 Toxicity Test: Pass the test

   Core Diameter: 70 to 76mm
  Max. Outer Diameter of Roll: 440mm

Suitability: 1.Winding of rolls should not be loose or telescopic. 

                             2. Rolls should be free from dents, creasing/wrinkles and      

                                damaged/collapsed core

                             3. Color of film should be uniform throughout

                             4. Thickness of film should be uniform
 Supply: Rolls should be individually wrapped in polythene film followed by   brown paper.       Rolls should be properly labeled with item name, quantity and supplied by information.

Storage: Store in air-conditioned room at temp. 20-30°C and at RH 45-65%.

